**Top-Coat**

**One layer of Hydro is 15-20 ml**

**(Regular Size Car)**

|  |
| --- |
| ***Preparation*** |
| **Controlled Environment:** - Ensure the application area maintains temperature and humidity control during and for at least 10 hours after application  **Washing and Decontaminating:**  - Clean your vehicle with an Iron remover to get rid of iron particles.  - Use a Mineral remover to remove mineral deposits. - Wash and decontaminate your vehicle using TAR remover  - If needed, use a clay bar to eliminate any tough contaminants.  **Polishing and Smoothing:**  - Compound and polish the vehicle to fix any imperfections and ensure a smooth surface. **Surface Prep:** -Highly recommended to use Titan Bioprep as it will enhance the bonding and remove any residue and silicon deposits.  -If you don’t have BioPrep:  Wash the car with dish soap solution and wipe down the car first with silicone remover (If polishing compound is silicone based).  -Use IPA to wipe down the surface. |

|  |
| --- |
| ***Application*** |
| **Product Application:**   * Apply enough drops of Hydro TX145 to your applicator and apply thickly. * Spread a puddle line and work in a crosshatch pattern slowly. * The size of the application area can be 50\*50cm panels or follow the bodylines of the car.   **Residue Removal:**   * Wipe off immediately with a new quality short pile microfiber until most residue is removed. * Follow up with a second short pile microfiber to ensure all residue is removed. * Buff with a new quality long pile microfiber.   **Final Inspection:**   * + Once applied and removed, inspect the surface with a long pile microfiber under a bright, diffused light source to ensure no residue remains.   **Layering:**   * + Apply the second layer of Hydro TX145 immediately after the first layer.   **Post-Application:**   * + Apply Ultra 4.0 after 2 hours.   + Do not expose your vehicle to the elements for at least 8 hours. * -Avoid washing the vehicle for the first 14 days to allow the coating to cure fully. |

***NOTES***

***Application Volume:***

***- Two layers of Hydro back-to-back average approximately 30ml.***

***Maintenance Schedule:***

***- Reapply Hydro every 2-3 years for optimal performance.***

***- Change your applicator and microfibers as needed to maintain quality application.***

***- Apply Ultra 4.0 every 3-6 months to enhance protection and gloss.***

***-If you are reskinning using Hydro after 2-3 years, then surface prep is a must before applying.***

***HANDLING***

***Store the coatings in the fridge, Recommended Temperature is 40-48 F.***

***Before Using: Take the coating out of fridge,***

***and let it set for 10-15 minutes and then Shake the bottle for 30 seconds before using.***

***All Coatings are based on elastomer technology***