**One layer of Hyper Glass for the WindShield is 5-10ml only**

|  |
| --- |
| ***Preparation*** |
| **Controlled Environment:*** Ensure the application area is temperature and humidity controlled during and for at least 10 hours after application.

**Wash and Decontaminate:*** Use a clay bar to remove hard-bonded contaminants from the glass.

**Glass Polish:*** Clean and prepare the glass surface with glass polish for further prepare.

**Wipedown:*** Wash the glass with a dishwashing solution.

**Final Wipedown:*** Highly recommended to use Titan Bioprep as it will enhance the bonding and remove any residue and silicon deposits.
* If you don’t have BioPrep:

 Wash the car with dish soap solution and wipe down the car first with silicone remover (If polishing compound is silicone based).* Use IPA to wipe down the surface.
 |

|  |
| --- |
| ***Application*** |
| **Apply the Coating:*** Apply 15-20 drops of Hyperglass to your applicator.
* Apply the product thickly.
* Reapply product to your applicator if it gets too dry during application.
* Apply only one layer of Hyperglass in a circular motion, followed by a crosshatch pattern.
* A second layer is not required and may compromise performance.

**Residue Removal:*** Remove the residue after 15-20 minutes.

**Exposure:*** Do not expose the glass to the elements for at least 10 hours.
* Do not wash the glass for the first 14 days.
 |

***NOTES***

***HANDLING***

**IR Lamp:**

An IR lamp can be used to speed up the curing process.

**Wiper Blades:**

* If the wiper blades are not new, replace them with a new set
* Coat the wiper blades with Hyperglass.

***Store the coatings in a cold, dry and dark place.***

***Before using, Shake the bottle for 30 seconds***

***Close the bottle after each use***