**Base-Coat
Stand Alone**

One layer of PX10 is 15-20 ml
(Regular Size Car)

|  |
| --- |
| ***Preparation*** |
| **Controlled Environment:**- Ensure the application area is temperature and humidity controlled during and for at least 10 hours after application.**Washing and Decontaminating:**- Clean your vehicle with an Iron remover to get rid of iron particles.- Use a Mineral remover to remove mineral deposits.- Wash and decontaminate your vehicle using a TAR remover.- If needed, use a clay bar to eliminate any tough contaminants.**Polishing and Smoothing:**- Compound and polish the vehicle to fix any imperfections and ensure a smooth surface.**Surface Prep:**- Highly recommended to use Titan Bioprep as it will enhance the bonding and remove any residue and silicon deposits.- If you don’t have BioPrep: Wash the car with dish soap solution and wipe down the car first with silicone remover (If polishing compound is silicone based).- Use IPA to wipe down the surface. |

|  |
| --- |
| ***Application*** |
| **Apply the Coating:*** Apply enough drops to your applicator and spread a thick puddle line.
* Work in a crosshatch pattern slowly.
* Cover an area of 50x50 cm or work with the body lines of the car.

**Immediate Wipe-Off:*** Immediately wipe off the coating with a new quality short pile microfiber until most of the coating is removed.
* Use a second short pile microfiber to remove all remaining residue.

**Buffing:*** Buff the area with a new high-quality long pile microfiber to ensure no residue remains.

**Final Inspection:*** Perform a final check with your long pile microfiber and a bright, diffused light source to confirm the surface is clean.

**IR Curing (optional):*** Cure every panel for 15 minutes at 60°C.

**Final Steps:*** Apply Ultra 4.0 after 2 hours if used as a standalone coating.
* Do not expose the vehicle to the elements for at least 8 hours.
* Do not wash the vehicle for the first 14 days.
 |

**Layering *(General Rules)*:**

Wait Two hours between the layers.

If PX10 is the base coat for Vulcan, wait 2 hours before applying Vulcan.

If PX10 is the base coating for Hydro, wait 2 hours before applying Hydro.

No need to IR cure topcoats like Vulcan and Hydro.

**Ultra 4.0:**

 Apply Ultra 4.0 before delivery.

***NOTES***

***HANDLING***

***Store the coatings in the fridge, Recommended Temperature 40-48 F.***

***Before Using: Take the coating out of fridge, and***

***let it set for 10-15 minutes and then Shake the bottle for 30 seconds before using.***

***All Coatings are based on elastomer technology***