**Base-Coat  
Stand Alone**

**One layer of Zeus is 15-20 ml**

**(Regular Size Car)**

|  |
| --- |
| ***Preparation*** |
| **Controlled Environment:**   * Ensure your vehicle is in a temperature and humidity-controlled environment during application and for at least 10 hours after.   **Washing and Decontaminating:**   * Clean your vehicle with an Iron remover to eliminate iron particles. * Wash and decontaminate your vehicle using a TAR remover. * Use a Mineral remover to get rid of mineral deposits. * If needed, use a clay bar to remove tough contaminants.   **Polishing and Smoothing:**   * Compound and polish the vehicle to fix imperfections and ensure a smooth surface.   **Surface Cleaning:**   * Highly recommended to use Titan Bioprep as it will enhance the bonding and remove any residue and silicon deposits. * If you don’t have BioPrep:   Wash the car with dish soap solution and wipe down the car first with silicone remover (If polishing compound is silicone based).   * Use IPA to wipe down the surface. |

|  |
| --- |
| ***Application*** |
| **Apply the Coating:**   * Apply enough drops of Zeus to your applicator and apply thick. * Spread the product in a puddle line, then use a crosshatch pattern to cover the area slowly. * Work in small sections, about 50x50 cm, or follow the car’s bodylines.   **Immediate Wipe-Off:**   * Immediately wipe off the coating with a new, high-quality short pile microfiber towel. * Use a second short pile microfiber towel to remove any remaining residue.   **Buffing:**   * Buff the area with a new, high-quality long pile microfiber towel.   **Final Inspection:**   * Check the surface with your long pile microfiber towel and a bright, diffused light to ensure no residue is left.   **IR Curing (optional):**   * Cure each panel with an infrared (IR) lamp at 60°C for 15 minutes.   **Final Touch:**   * Apply Ultra 4.0 if Zeus Dark Matter is being used as a standalone product.   **Post-Application:**   * Do not expose your vehicle to the elements for at least 12 hours. * Do not wash the vehicle for the first 14 days. |

**Layering *(General Rules)*:**

Wait Two hours between the layers.

**If applying Hydro as a topcoat, wait 2 hours.**

No need to IR cure topcoats like Hydro.

**Ultra 4.0:**

Apply Ultra 4.0 before delivery.

**Change applicator and microfiber towels as needed to maintain application quality.**

***NOTES***

**HANDLING**

***Store the coatings in the fridge, Recommended Temperature is 40-48 F.***

***Before Using: Take the coating out of fridge,***

***and let it set for 10-15 minutes and then Shake the bottle for 30 seconds before using.***

***All Coatings are based on elastomer technology***