**Base-Coat
Stand Alone**

**One layer of Zeus is 15-20 ml**

**(Regular Size Car)**

|  |
| --- |
| ***Preparation*** |
|  **Controlled Environment:*** Ensure your vehicle is in a temperature and humidity-controlled environment during application and for at least 10 hours after.

**Washing and Decontaminating:*** Clean your vehicle with an Iron remover to eliminate iron particles.
* Wash and decontaminate your vehicle using a TAR remover.
* Use a Mineral remover to get rid of mineral deposits.
* If needed, use a clay bar to remove tough contaminants.

**Polishing and Smoothing:*** Compound and polish the vehicle to fix imperfections and ensure a smooth surface.

**Surface Cleaning:*** Highly recommended to use Titan Bioprep as it will enhance the bonding and remove any residue and silicon deposits.
* If you don’t have BioPrep:

 Wash the car with dish soap solution and wipe down the car first with silicone remover (If polishing compound is silicone based).* Use IPA to wipe down the surface.
 |

|  |
| --- |
| ***Application*** |
| **Apply the Coating:*** Apply enough drops of Zeus to your applicator and apply thick.
* Spread the product in a puddle line, then use a crosshatch pattern to cover the area slowly.
* Work in small sections, about 50x50 cm, or follow the car’s bodylines.

**Immediate Wipe-Off:*** Immediately wipe off the coating with a new, high-quality short pile microfiber towel.
* Use a second short pile microfiber towel to remove any remaining residue.

**Buffing:*** Buff the area with a new, high-quality long pile microfiber towel.

**Final Inspection:*** Check the surface with your long pile microfiber towel and a bright, diffused light to ensure no residue is left.

**IR Curing (optional):*** Cure each panel with an infrared (IR) lamp at 60°C for 15 minutes.

**Final Touch:*** Apply Ultra 4.0 if Zeus Dark Matter is being used as a standalone product.

**Post-Application:*** Do not expose your vehicle to the elements for at least 12 hours.
* Do not wash the vehicle for the first 14 days.
 |

**Layering *(General Rules)*:**

Wait Two hours between the layers.

**If applying Hydro as a topcoat, wait 2 hours.**

No need to IR cure topcoats like Hydro.

**Ultra 4.0:**

 Apply Ultra 4.0 before delivery.

**Change applicator and microfiber towels as needed to maintain application quality.**

***NOTES***

**HANDLING**

***Store the coatings in the fridge, Recommended Temperature is 40-48 F.***

***Before Using: Take the coating out of fridge,***

***and let it set for 10-15 minutes and then Shake the bottle for 30 seconds before using.***

***All Coatings are based on elastomer technology***